|  | Document # | Date Effective |
| --- | --- | --- |
|  | LAT-PS-00880-02 | Draft |
|  | Author: | Supersedes |
|  | A. Brez | none |
| LAT Technical Document |  |  |
|  | Subsystem/Office |
|  | Tracker Subsystem |
| Document Title |
| Production and tests of the working ladders for the GLAST Engineering Model Tower |

CHANGE HISTORY LOG

| Revision | Effective Date | Description of Changes |
| --- | --- | --- |
| 2 | September 7, 2002 | Added figures and text for encapsulation results. R. Johnson |

# PURPOSE

This document describes the results of the production of 32 ladders consisting of working “GLAST2000” wafers. These ladders will instrument 4 trays that will be used to fully test the operational limits of the GLAST silicon Tracker.

# SCOPE

The ladders have been produced following the procedure described in LAT-PS-635 that derives from the BTEM assembly experience (1-2). The procedure defines the methods used   assemble, test and qualify the flight ladders starting from 4 GLAST2000 SSDs. The 4 SSDs are glued together head to head without any mechanical structure, and all the pads are wire bonded in series to form a unique sensor 358mm long, 89.5mm wide. The wire bonds are encapsulated to avoid short circuits due to conductive dust or chips. This production test will be used to certify the assembly, mechanical and electrical test procedure.

# DEFINITIONS

AC Pad	Pad to access the Al metal electrode on the strips

Dam&Fill	Encapsulation technique. A thixotropic dense adhesive is used as a dam to contain a second fluid adhesive that encapsulates the wire bonds.

Encapsulation  Adhesive covering of the wire bonds and metallic pads to prevent short circuits or electrical discharges

ESD	Electro Static Discharge

Ladder	Assembly of 4 SSDs edge bonded in series, with strips connected by wire bonding.

N-sub	Substrate contact on the detector front.

Pad	Area of the Al metal layer accessible through the passivation layer.

The pad area is defined as the bondable area.

Pitch	Distance between strip centers (228m)

Rms	Root mean square

SSD 	Silicon Strip Detector

Tray	Flat composite panel that supports the SSD ladders, readout electronics, and converter foils in the TKR mechanical structure

Tower	Assembly of 19 trays, stacked vertically and held together with sidewalls, to form one TKR detector module

(m	Micro meter (10-6meter)

# REFERENCES

- SLAC Pub 8682, Beam Test NIM Paper

- NIM A 457, p. 128, Assembly of BTEM Tracker

- LAT-TD-00011, GLAST LAT Silicon Detector Specification

- LAT-TD-00527, LAT Tracker SSD Dimensional and Electrical Inspection Procedure

- LAT-MD-00228, LAT Calorimeter, Tracker, and Data Acquisition Contamination Control Plan.

- LAT-PS-00635, Flight ladder assembly procedure

- LAT-TD-00879,	Production and measurements of the mechanical ladders for the GLAST Engineering Model Tower

- LAT XXY, Results of the SSDs testing

- articolo francesco

# The Silicon Strip Detectors and Ladders

The SSDs were produced by Hamamatsu Photonics following the requirements of Ref. [3].  All the SSDs used in this production run were accepted by INFN following the procedure of Ref. [4].  The wafers were assembled into ladders, wire bonded and encapsulated following the procedure of Ref. [6].

# Alignment results

The ladders were produced using a set of 12 ladder assembly jigs (Fig. 1).  On each ladder data-sheet the serial number and the serial number of the relative jig was reported.  The alignment of the wafer is mechanical, made by pushing each wafer against the Teflon coated references of the jig.  With a Computerized Measurement Machine (CMM), with 5 mm maximum error, the alignment of the ladders was checked by measuring the positions of the cross-shaped “B” markers placed at the corners of the SSDs (see Figs. 2 & 3).

On each ladder, 8 points (2 per wafer, close to the extremity) were measured, and the residuals from the best-fit straight line were calculated.  Fig. 4 shows the distribution of the residuals, which have a 3.6 (m rms.  That should be compared with the 5.5 (m rms obtained in the mechanical ladder production [7].  These excellent results are due to the very good dicing precision (1.3 (m rms) of the SSDs from Hamamatsu Photonics (Refs. [8], [9]).

Fig. 5 shows the distribution of the thickness of the adhesive-joint between SSDs. The joint thickness was calculated as the distance between the “B” markers on two adjacent SSDs minus 0.6 mm.  The mean joint thickness is 31 (m.

Figure 1.  Ladder assembly jig.

Figure 2.  Ladder scheme.

Figure 3. The cross-shaped reference “B” markers.

Figure 4.  Residuals from the best-fit straight line through the 8 “B” marker centers.

Figure 5.  Distribution of the adhesive joint thickness.

# Electrical test results

The ladders were tested electrically on a PA200 Suss Microted probe station with a custom chuck designed to accept the ladders.  The detailed description of the procedure and of the test is in Ref. [6].

The leakage currents measured before encapsulation are on average 1.8 times the sum of the leakage currents measured by INFN on the SSDs that form the ladder (Fig. 6).  One ladder (ID 23) had a leakage current of 10 A.  After optical inspection a grain of organic material was found covering the gap between guard ring and bias ring.  After partial cleaning of the organic residual, the leakage current of this dropped to 4 A, indicating that the anomalously high leakage current was induced by the contaminant.

The SSDs are shipped in a paper envelope.  Inside the envelope the SSD are sandwiched between two cardboard foils.  We have observed that the presence of dust, of fibers and of organic material, is due to residue from the two cardboard foils.  Following this observation, an improved inspection and cleaning operation will be implemented at the assembly factory.  The SSDs will be inspected under a binocular microscope and flushed in the direction of the strips from one side to the other side with ionized Nitrogen flow to remove dust and fibers.  If remaining organic material is observed, the SSD will be gently cleaned with isopropyl alcohol and wiped with a second dry swab.

The SSDs that form a ladder have been selected such that their depletion voltages falls within a 10 Volt range.  The depletion voltage of the ladders assembled so far is very close to the average of the depletion voltages of the 4 SSDs (Fig. 7).

The leakage currents of two of the ladders was monitored for 26 hours.  The stability during this period was approximately (20% (see Fig. 8).

The wire-bonding quality was checked by applying a 100 V step to the AC pads via a resistor and studying the RC response.  This test of the AC pads indicated no missing wire bonds.  This test did recognized 12 of the 14 AC strips that were known prior to ladder assembly to be shorted to the substrate plus 4 additional instances of shorted strips.  If we assume that these 4 instances are due to the wire bonding, then we have a probability of breaking the insulator during wire bonding equal to 1/5760.  This is an acceptable level given our goal of no more than 2% non-working strips in the final assembly.

Figure 6: Ladder leakage current at 150V.

Figure 7: Depletion voltage of the ladders (red squares) and average values of the depletion voltages of the SSDs from which each ladder was made (blue line).

Figure 8: Leakage current stability of ladders #0026 and #1001.

# TEsts After Encapsulation

Three of the engineering-model ladders were encapsulated with Dow Corning 3145RTV for the dam and GE 615 RTV for the fill.  The following figures show preliminary results from testing those ladders electrically following the encapsulation.

Figure 9, AC strip currents at 100V DC before and after encapsulation.

Figure 9 shows results of a test of the AC strip currents at 100V DC both before and after encapsulation.  There is a spread of the values, but the maximum is less than 4 nA, showing very good insulation of the encapsulation.  This means that the tests procedure to detect an AC short is still valid.

Figure 10.  Leakage current of ladder before and after encapsulation.

Figure 10 shows that there is some confusion with the leakage current data after encapsulation.  In two cases (9 and 12) there is a significant decrease of current after encapsulation.  The decrease could be due to long time constants commonly seen in SSDs.  Take the ladder with ID 23, for example.  It had a leakage current of 10 (A just after assembly, 2.5 (A after cleaning of a spec of dirt, and now after 1 month of storage has only 1.0 (A of leakage current.  In any case, all of the examples shown in Figure 10 are well within the acceptance range after being encapsulated.

Figure 11.  Leakage current monitoring of a cutoff SSD covered with GE-615 RTV.

In addition to the ladder tests, a small detector from the GLAST-2000 cutoffs was covered with the fill material and is being monitored long-term.  Figure 11 shows the measured leakage current, corrected for temperature variations.

# Conclusion

The ladder assembly procedure was demonstrated to meet or surpass the LAT Tracker requirements by fabrication and test of a set of live ladders destined to be used in the Tracker Engineering Model.  A problem of high leakage current was found in a few ladders to be due to surface contamination of the SSDs caused by the packaging material.  An extra cleaning step was instituted to solve this problem with the existing SSDs, and use of an alternative packaging material is under investigation for the remaining SSD production.

# Text boxes

Vacuum chucks

Pistons

Mechanical references