# LAT X-LAT Peer Review RFA Response #5

Action Requested:

1) Provide some level of detail of the bonding (Nusil) of the heat pipes to the X-LAT plate. How achieve 10 mil thickniess of Nusil? Rivet w/Nusil cured or wet? How verify appropriate pressure on Nusil to achieve necessart thermal conductance? 2) Consider enforced displacements of X-LAT plate during T/V testing to simulate non-planarity of E-Box interface.

Reason:

1) Discussions at the review did not clear up this level of detail.

2) Concern that distorted X-LAT plate might affect thermal conductance of joint.

Response:

Heat pipes will be bonded using wires to control bondline thickness. A development test was performed to verify the process. The steps were:

- Prepare mating surfaces (per specs)

- Apply 0.008” thick Teflon tape to the X-LAT plate around the perimeter of the heat pipe.

- Install 0.0045” diameter wire to the plate on each side of the heat pipe lengthwise. The wire is to be outside the rivet locations (Note: the rivet holes in the  X-LAT plate and the X-LAT heat pipe are matched drilled prior to these bonding operations).

- Apply Nusil CV-2942 adhesive to the plate. Use a stiff squeegee across the Teflon tape to spread a 0.008” adhesive layer on the plate.

- Install the heat pipe on the plate and install all rivets within the adhesive pot life.

- Clean up squeeze out and remove Teflon tape.

- The results were a fairly uniform 0.0065” thick bondline. The minimum thickness was 0.0031” next to a rivet and 0.0093” thick halfway between (lengthwise) two rivets. Since this is primarily a thermal bond, these variations are acceptable.